## Dataset list

18Ni300 maraging steel

## Related Links, Article: https://doi.org/10.1016/j.ijfatigue.2025.109023

Published: 5 June 2025|Version 1|DOI:10.17632/sfkgmjnf37.1

Contributors:

Aleksander Karolczuk,

Andrzej Kurek

## Description

The provided Excel file contains the experimental data used in the study: Karolczuk, A., & Kurek, A. (2025). Machine learning insight into the mean stress impact on fatigue life of additively manufactured 18Ni300 maraging steel under various multiaxial stress paths. International Journal of Fatigue, 198, 109023. https://doi.org/10.1016/J.IJFATIGUE.2025.109023. The dataset includes fatigue life results for thin-walled cylindrical specimens made of 18Ni300 maraging steel, produced by Laser Powder Bed Fusion (LPBF). The specimens were tested in the as-built condition (no machining) following a standard ag,,ddbing heat treatment. Fatigue experiments were performed under 22 different axial-torsional stress paths, covering in-phase, out-of-phase, and mean-stress conditions. Tests were carried out using constant-amplitude, sinusoidal loading under force- or torque-control in accordance with ISO 1099. Two testing systems were employed: Instron Electropuls E10000 and Instron 8852. All specimens were tested to complete fracture (separation).

## Link on Mendeley platform: https://data.mendeley.com/datasets/sfkgmjnf37/1

# CuZn37

# multiaxial fatigue data Published: 25 October 2021|Version 1|DOI:10.17632/7fbkf6y7gv.1

Contributors:Łukasz Pejkowski,Dariusz Skibicki,Aleksander Karolczuk

## Description

The file contains experimental data on the strain-controlled multiaxial fatigue tests of CuZn37 brass. It includes also the input data for the fatigue life prediction based on the Gaussian process regression.

## Institutions

- Uniwersytet Technologiczno-Przyrodniczy im Jana i Jedrzeja Sniadeckich w Bydgoszczy

- Politechnika Opolska

## Categories

Multiaxial Fatigue, Fatigue Life Prediction, Low-Cycle Fatigue, Fatigue Life, Gaussian Process

## Related Links

Article

https://www.sciencedirect.com/science/article/pii/S0142112317301901

Article

https://www.sciencedirect.com/science/article/pii/S0142112317301901

Article

https://onlinelibrary.wiley.com/doi/full/10.1111/ffe.12854

Article

https://onlinelibrary.wiley.com/doi/full/10.1111/ffe.12895

## Link from Mendeley platform: https://data.mendeley.com/datasets/7fbkf6y7gv/1?utm_source=chatgpt.com